## Slide 1
SCIANTIX «Past»
SCIANTIX Present
SCIANTIX Future
Challenges
Davide Pizzocri
Lyon and online, 15.05.2024

## Slide 2
Object, nuclear fuel pin
Cladding
Fuel
Helium gap
Nuclear fuel rod (ThR//FR) is made of a stack of oxide (UO2//MOX) fuel pellets wrapped in metallic (Zry//SS) cladding
Its performance is fundamental for safe operation of the reactor (and licensing and design)
Need of integral fuel performance codes (FPCs) and integral irradiation experiments to assess the fuel rod thermo-mechanical behaviour (σ,ε, and T)
Focus on inert gas behavior, i.e.,
gaseous swelling & fission gas release

## Slide 3
Horizon Europe (2023-2027, 300k€)
WP leadership (V&V)
Involved in code development, V&V, UA&SA, ML
Obj Developement of open source tools for nuclear fuel simulation
Ongoing activities
  Data assimilation / ANN
  Qualification standards
  Integral validation
OperaHPC
TRANSPARANT
Horizon Europe (2024-2028, 400k€)
WP leadership (code development)
Involved in support to experimental design, code development, …
Obj Development of actinide bearing fuels and technologies
Planned activities
  Thermochemistry
  Material properties
  Radioactive fission products

## Slide 4
Multi-scale modelling approach
Next talks
M. Bertolus
A. Scolaro
Goal. Simulation of integral experiments (IFPE) at engineering//reactor-scale
Goal. Modelling at grain-scale and assessment (by separate effect experiments)
SCIANTIX. Grain-scale code, for model development and V&V

## Slide 5
Physics-based modelling is fundamental in order to act as bridge between different scales
Can be informed by lower-length scale calculations and experiments, in terms of physical phenomena and model parameters
Need to overcome correlation-based approaches currently used in FPCs
Low computational time is needed for effective use within fuel performance codes
IGB model called at each thermo-mechanical iteration, in each time-step of the FPC simulation, in each mesh point
The huge number of calls implies that numerical robustness is a requirement
BISON
Cladding
Fuel
Helium gap
Multi-scale modelling approach, requirements

## Slide 6
Developed at Politecnico di Milano
It is a 0D stand-alone code, designed to be included as a mechanistic fission gas behaviour module in existing fuel performance codes
Constitutes the natural environment for the development, verification, and validation of fission gas behaviour models, and for the simulation of separate-effect test experiments
It can be included in existing multiphysics platforms and fuel performance codes as a module (via simple interface) to evaluate fission gas release and gaseous swelling or can be used as stand-alone
Available as open-source software (MIT license)
Multi-scale modelling approach, requirements

## Slide 7
Diffusion
Re-solution
Trapping
Generation of fission gases (Xe, Kr)
Fission reactions
Intra-granular bubble swelling
Inter-granular gas
(lenticular bubbles)
Intra-granular gas
(small & coarsened bubbles)
Intra-granular gas (single atoms)
Grain-boundary saturation and/or micro-cracking
Fission
gas release
Inter-granular bubble swelling
High burnup structure
The SCIANTIX code, physical aspects

## Slide 8
State of the Art. Correlations for bubble radius and bubble concentration, f(T)
Baker, J. Nucl. Mater., 1977
Govers et al., J. Nucl. Mater., 2012
0.1 ps
0.5 ps
1.0 ps
2 nm
Lower length-scale information available
Bubble nucleation appears to be driven by fission fragments
Bubble re-solution appears to be (mainly) heterogeneous and again driven by fission fragments
Applicative modelling example
Intra-granular bubble evolution

## Slide 9
Physically-based single-size model derived from cluster dynamics
Fokker-Planck expansion in the phase space, at order zero
Assumption of first moment expansion implies single-size model and is valid for peaked distributions (confirmed from LLS)
All clusters with size n > 2 are considered immobile and counted as bubbles
Applicative modelling example
Intra-granular bubble evolution

## Slide 10
Separate effect validation performed in SCIANTIX: good agreement with experimental data
UA & SA with respect to model parameters via Total Monte Carlo (low computational time)
Data from Baker, 1977. JNM
Applicative modelling example
Intra-granular bubble evolution, separate effect validation

## Slide 11
Grain-boundary bubbles growth by vacancy absorption and coalescence
A saturation value of the fractional coverage of the grain-faces is considered
At saturation, further bubble growth
is compensated by gas release
+ Grain-boundary micro-cracking
Fc increases
Fc = constant (FGR occurs)
Saturation
Pastore et al., 2013, NED
Inter-granular bubble evolution

## Slide 12
White et al., 2006
Inter-granular bubble evolution, separate effect validation

## Slide 13
The SCIANTIX 2.0 flowchart
External shell (right) representing the coupling with fuel performance codes (TRANSURANUS, OFFBEAT, …)
Meso-scale module (left) containing physical / behavioural models
  construction of specific objects for IGB modelling
  definition of solvers (robust numerics)
  simulation = models + solvers
  V&V continuous activities, matrix of cases for non-regression tests

## Slide 14
The SCIANTIX 2.0 inheritance diagram

## Slide 15
The SCIANTIX 2.0 inheritance diagram
Helium
in UO2 / MOX
Helium behaviour
Production
Diffusion
Solubility
Interaction with fission gases  bubbles

## Slide 16
The SCIANTIX 2.0 inheritance diagram
Cs, I, Te, … in …
CsI, … in …
Interaction with thermochemistry module
Useful for experimental design (source term estimation)
Step towards JOG models

## Slide 17
The SCIANTIX 2.0 inheritance diagram
Connected to fuel microstructure (e.g., High Burnup Structure)
Connection to material properties
Use of advanced modelling techniques (surrogate modelling)

## Slide 18
Ongoing model development
Athermal release

## Slide 19
Ongoing model development
Athermal release

## Slide 20
Ongoing model development
Athermal release

## Slide 21
Ongoing model development
Dislocation density

## Slide 22
Ongoing model development
Dislocation density

## Slide 23
Ongoing model development
Dislocation density, surrogate model

## Slide 24
As models become more and more physics-based and accurate in representing the phenomena of interest, the computational requirements rises
  Room for applying machine learning and artificial intelligence methodologies
  Challenge of explainability of such methods
As SCIANTIX use is more and more relevant in engineering calculation, the quality assurance of the code becomes a priority
  Activities ongoing in the OperaHPC project and in other international frameworks
  Effort in involving in the team non-nuclear profiles
As the framework for research activities on nuclear material changes (e.g., CONNECT-NM) thekey features of SCIANTIX can open up opportunities
  Accelerated qualification of nuclear fuels (fast transfer of knowledge along scales)
  Extension to other nuclear materials
Conclusion and Future challenges

## Slide 25
Thank you all for your kind attention !

## Slide 26
Exchanges
Self-introduction
Contributions from new users
New development of interest
Intention for future proposals
Davide Pizzocri, Lelio Luzzi
Lyon and online, 15.05.2024

## Slide 27
SCIANTIX is at a sweet spot in the multi-scale modelling and calculation chain
The inclusion of SCIANTIX in fuel performance codes is fairly easy (depending on the targeted application)
The transfer of info/data from lower-length scales is direct
Summary
FPCs
FPCs
Lower-length scales
Meso-scale
Separate effect

## Slide 28
SCIANTIX is a meso-scale tool originally developed for the simulation of inert gas behaviour in oxide fuels
It has a flexible structure and can be extended towards other fission products and other fuel materials
Each model in SCIANTIX is validated based on separate effect tests
Summary
Athermal release
 SMRs, DH
Dislocation density
 SMRs, DH
???
Helium
 FRs, storage
Fuel fragmentation
 Accidental conditions
Doped fuels
 ATF, SMRs
Fission product behaviour  JOG
Other materials ???

## Slide 29
As models become more and more physics-based and accurate in representing the phenomena of interest, the computational requirements rises
  Room for applying machine learning and artificial intelligence methodologies
  Challenge of explainability of such methods
As SCIANTIX use is more and more relevant in engineering calculation, the quality assurance of the code becomes a priority
  Activities ongoing in the OperaHPC project and in other international frameworks
  Effort in involving in the team non-nuclear profiles
As the framework for research activities on nuclear material changes (e.g., CONNECT-NM) thekey features of SCIANTIX can open up opportunities
  Accelerated qualification of nuclear fuels (fast transfer of knowledge along scales)
  Extension to other nuclear materials
Conclusion and Future challenges